NEW MATERIALS BASED ON NATURAL ZEOLITES USED

IN THE FILTRATION OF UNDERGROUND WATER

Rodica Pode*, Georgeta Burtică*, Sidonia Herman** and Aurel Iovi*

*“Politehnica” University Timişoara, Faculty of Industrial Chemistry

and Environmental Engineering, Victoriei Sq. 2, 1900 Timişoara, România,

**S C AEM - SA Timişoara, 1900 Timişoara, Romania.

# INTRODUCTION

In Romania most of the undergroud waters contain about 3 mg Fe/dm3 and 1 mg Mn2+/dm3. Their utilisation for preparing drinking waters presumes the elimination of iron and manganese to levels below 0.05 mg/dm3.

The experimental research carried out with waters with a variable content of calcium, magnesium, iron and manganese have showed that the natural zeolites chemically activated either as the acid form (Z-H) or the sodium one (Z-Na) achieve in a fair extent the elimination of the metal ions from water by an ion-exchange process1-2.

For the undergroud waters the most important problem is not the elimination of the hardness, but that of the retention of the iron and manganese ions.

From the literature there are partially known the results of the experimental work of Tarasevich et  al.3-4, Polyak et al.5, which used manganesed clinoptilolite, in order to retain iron and manganese from waters.

Consequently, the experimental research of the present paper aimed at the utilisation of Romanian natural zeolite as support for a manganese combination, as well as at the efficiency of the obtained material in the processes of elimination of iron and manganese.

# EXPERIMENTAL

1. The mineralogical and chemical characterization of the natural zeolite.

This research used natural zeolite ore originated from Bârsana (Maramureş county).

Its mineralogical composition has been determined by X-ray diffraction using a Dron 3 instrument, with the radiation Cu K.

2. Obtaining and characterization of the manganesed zeolite.

The natural zeolite, with the grain size in the range 315-500 m, has been subjected in the first stage to a chemical  activation in order to increase the ion exchange capacity. The zeolite has been subsequently  treated  with  a  2M  solution  of  MnCl2, at a ratio solid:liquid of 1:4, for 3 hours. After

decantation  and filtration, the material has been treated with a KMnO4 solution of 5g/L concentration for 3 hours. The obtained product was washed in order to remove the excess of KMnO4 and dried at 105C for 6 hours.

The samples of manganese zeolite have been subjected to chemical analysis determining the content of manganese before and after the oxidation with KMnO4.

3. Research concerning the utilization of the manganesed zeolite in the process of     elimination of iron and manganese from waters.

These studies were carried out in dynamic regime, in closed laboratory columns of 10 mm diameter and 200 mm height, each equipped with 4 grams of zeolite material. There have been used manganesed zeolite (Z-MnO2) and clinoptilolitic zeolite activated as the sodium state (Z-Na), of 315-500 m grain size.

For the determinations have been used synthetic waters with different contents of Fe2+ and Mn2+. It has been used a specific loading of 20m3/m2h, maintaining during the operating cycle a constant level above the zeolite layer of 30 mm. Effluent samples of 0.4 L were collected and analyzed. The concentration of the iron and manganese ions has been determined by atomic absorption spectrophotometry.

# RESULTS AND DISCUSSION

1. Mineralogical and chemical characterization of the natural zeolite.

There are evidenced some diffraction signals, at angles, respectively interplane distances that are characteristic for clinoptilolite, according to data from the ASTM cards 25 – 13,49. Other minerals are also evidenced, such as albite and -quartz6.

By measuring the intensity of the spectral lines from the diffraction spectrum and comparing it with those of pure clinoptilolite, it has been determined an average clinoptilolite content in the zeolite ore of about 68%.

The average chemical composition of the zeolite ore (% weight) was : SiO2 62.11, Al2O3 13.2,Fe2O3 2.20, CaO 3.56, MgO 1.11, K2O 2.55, Na2O 1.28, TiO2 0.30, P2O5 0.05, MnO 0.06, calcination losses 8.66. From these data have been determined for the studied zeolite ore a SiO2/Al2O3 ratio of 5.12, respectively a Si/Al ratio of 4.49, values that are characteristic for clinoptilolite.

2. Characterization of the manganesed zeolite.

The process of manganese doping may be expressed by the chemical equation :

(7 - 2x)Mn2+ + (2x - 2)MnO4- + (8 - 3x)H2O  5MnOx + (16 - 6x)H+   (1)

where x is the average oxidation index of manganese. This is defined according to the relation :

7−2x5=Mni2+−Mnf2+Mnt−Mnf2+                 (1)

where : Mni2+- the initial content of Mn2+ in the zeolite after treatment with the 2M

solution of MnCl2 (7.50 mg/g) ;

Mnf2+ - the final content of Mn2+ in zeolite found after the oxidation with

KMnO4 (2.10 mg/g) ;

Mnt - the overall content of Mn2+ and Mn4+ in the zeolite (9.8 mg/g).

It follows that it has been obtained manganese zeolite of about 10 mg Mn/g and an average oxidation index of 1.75.

3. Research concerning the utilization of the manganesed zeolite in the process of elimination of iron and manganese from waters.

The results obtained concerning the retention of iron on sodium state zeolite (Z-Na) , at concentrations of 1, 3, and 5 mg/dm3, respectively of manganese zeolite, are presented in Figure 1 and Figure 2.

Figure 1. Iron retention on Z-Na versus the specific volume of influent.

Figure 2. Iron retention on Z-MnO2 versus the specific volume of influent.

One may observe from both the above figures a diminishing in time of the retaining capacity, which can be explained by the exhaustion of the ion-exchange capacity for Z-Na, respectively the decrease of the oxidation capacity of the MnO2 layer and the accumulation of insoluble iron oxides clogging the zeolite material.

The total amount of iron retained on the two types of zeolites is presented in Table 1.

Table 1. Retaining capacity for Fe2+  on Z-Na and Z-MnO2 at different iron concentrations

in the influent.

| Crt. No. | Fe2+ concentration (mg/L) | Retaining capacity (mg/g zeolite) |  |
| --- | --- | --- | --- |
|  |  | Z-Na | Z-MnO2 |
| 1 | 1 | 1.06 | 2.66 |
| 2 | 3 | 3.90 | 7.05 |
| 3 | 5 | 4.98 | 10.90 |

It may be observed the doubling of the iron amount retained on the manganesed zeolite.

The results obtained for the elimination of Mn2+ from waters with different initial concentrations are presented in Figure 3.

Figure 3.Retaining capacity for Mn2+  on Z-Na and Z-MnO2 at different manganese

concentrations  in the influent.

Mn2+ is retained on Z-Na, like in the case of iron, by ion exchange. On Z-MnO2 it takes place a complex process of ion exchange and oxidation of Mn2+ by MnO2, with the formation of insoluble oxides. The total amount of Mn2+ retained on the two types of zeolites is presented in Table 2.

Table 2. Retaining capacity for Mn2+  on Z-Na and Z-MnO2 at different manganese

concentrations  in the influent.

| Crt. No. | Mn2+ concentration (mg/L) | Retaining capacity (mg/g zeolite) |  |  |
| --- | --- | --- | --- | --- |
|  |  | Z-Na | Z-MnO2 |  |
| 1 | 1 | 2.30 | 2.61 |  |
| 2 | 3 | 2.71 | 3.78 |  |
| 3 | 5 | 3.05 | 4.66 |  |

# CONCLUSIONS

The X-ray studies, as well as those concerning the chemical composition, evidenced that the most important component of the Bârsana zeolite ore is clinoptilolite (about 68%).

From this raw-material there has been obtained a manganesed zeolite with a content of 10 mg/g and an average oxidation index of 1.75.

For the synthetic waters prepared it has been established that the manganesed zeolite exhibited a higher retaining capacity than that of the Z-Na state, for both iron and manganese. The process of retaining iron and manganese is a complex one, consisting of ion-exchange, oxidation and filtration of the two cations.

# REFERENCES

- Burtică, G., Pode, R., Herman, S. and Jitea, V., Studies Concerning the Possibility of Iron and Manganese Removing from the Underground Waters by means of Native Natural Zeolite, Ann. West Univ. Timişoara, Ser. Chem., No. 2, pp. 1 – 10, 1994.

- Burtică, G., Pode, R., Herman, S. and Jitea, V., Double Filtering of Iron and Manganese out of Underground Waters by using Native Natural Zeolite, Ann. West Univ. Timişoara, Ser. Chem., No. 3, pp. 1 – 7, 1994.

- Tarasev ich, Y. I., Use of Clinoptilolite in the Purification of Natural Waters, Program and Abstracts : Zeolite ‘93 - 4th International Conference on the Occurence, Properties and Utilisations of Natural Zeolites, Idaho, 1993, pp. 199 – 201.

- Tarasevich, Y. I., Polyakov, V. E. and Polyakova, I. G., Preparation of Modified Adsorbent Based on Clinoptilolite and its Application for the Demanganation of Artesian Drinking Water, Zeolite ‘97 - 5th International Conference  on the Occurence, Properties and Utilisations of Natural Zeolites, Ischia, Naples, 1997, pp. 282 – 284.

- Polyak, K., Hlavay, J. and Maixner, J., Surface Properties of MnO2 Adsorbent Prepared on Natural Clinoptilolite, Program and Abstracts : Zeolite ‘93 - 4th  International Conference  on the Occurence, Properties and Utilisations of Natural Zeolites, Idaho, 1993,   pp. 165 – 167.

- A. S. T. M. Cards : 25 – 1349; 19 – 1184; 33 – 1161.